[image: image1.emf]



� EMBED AcroExch.Document.7  ���








[image: image2.emf]_1637478896.pdf


DUCTILE IRON MECHANICAL JOINT CONNECTOR   


PRODUCT SPECIFICATIONS


SIZE RANGE: •	 3” - 36”


MATERIAL: •	 MJ x MJ Connector and Spacers manufactured from high strength ductile iron in accordance 
with ASTM A536 Grade 65-45-12.


PRESSURE RATING: •	 350 PSI Water Working Pressure 3” - 24”
•	 250 PSI Water Working Pressure 30” & 36”


TESTING: •	 Manufactured in accordance with ANSI/AWWA C153/A21.53 and ANSI/AWWA C110/A21.10
•	 All fittings are hydrostatically tested in accordance with SIGMA Quality Management Standard
•	 All fittings are heat coded to ensure traceability and verification of metallurgical properties in 


accordance with the prevailing standards and SIGMA Quality Management Standards.


COATING: •	 Interior and exterior of fitting is e-coated


GASKETS: •	 SBR in accordance with ANSI/AWWA C111/A21.11


T-BOLTS: •	 Low Alloy corrosion resistant high strength steel in accordance with ANSI/AWWA C111/A21.11


EYE-BOLTS: •	 Low Alloy corrosion resistant high strength steel in accordance with ANSI/AWWA C111/A21.11


STANDARDS: •	 Certified to NSF61 Standard
•	 ANSI/AWWA C153/A21.53 Ductile Iron Compact Fittings


INSTALLATION: •	 Per ANSI/AWWA C600 Standard Installation of Ductile-Iron Mains and Their Appurtenances


December 2016 SIGMA Corporation  www.sigmaco.com






